## Slide 1: LID-QMS areal fuel retention at end of JET operations 19 & 20 December 2023
Assumptions:
AMU4 calibration factor used for AMUs
19/12/2023 AMU4 calibration factor used for 20/12/2023 data points
Calibration = Jump method

## Slide 2: Assumptions
Area of laser raster is approximate
Gas calibrations from 19th December for AMU4
  No calibration for 20th December
  No scaling for AMU3, 5, 6
AMU converted to atoms
  AMU2 = 2 x H
  AMU3 = 50:50 H:D
  AMU4 = 2 x D
  AMU5 = 50:50 D:T
Jump method for data analysis and calibration factor
  Started to apply 3
  Any jumps < 3 considered limit of detection
No pumping of calibration gas puffs…see Gennady’s presentation later
4 x 4
1.5 mm step in x & y
~0.563 cm2
5 x 2
1.5 mm step in x & y
~0.405 cm2
4 x 4
1.5 mm step in x
1.0 mm step in y
~0.45 cm2

## Slide 3: HFGC LH14W

## Slide 4: HFGC LH14W Poloidal
4 x 4
1.5 mm step in x & y
~0.563 cm2
Area used is large  areal retention will increase
Ratio of RGA5 D/T very uniform  issue with data?
All data collected on 19th December

## Slide 5: HFGC LH14W Poloidal
Deuterium only
Indicative retention from previous post-mortem
Lots of caveats….

## Slide 6: HFGC LH14W Toroidal
Deuterium only
4 x 4
1.5 mm step in x & y
~0.563 cm2
5 x 2
1.5 mm step in x & y
~0.405 cm2

## Slide 7: HFGC LH14W Toroidal
T/(H+D+T) %
4 x 4
1.5 mm step in x & y
~0.563 cm2
5 x 2
1.5 mm step in x & y
~0.405 cm2

## Slide 8: AMU4/AMU5 for RGA5 and RGA7
RGA7: AMU4 > x10 AMU5
RGA5: AMU4 ~ x2 AMU5
Why the difference between RGA5 & RGA7
 Issues with RGA5 data?

## Slide 9: T/(HDT) % for RGA5 and RGA7
Why the difference between RGA5 & RGA7
 Issues with RGA5 data?

## Slide 10: 14IWG1B

## Slide 11: 14IWG1B Poloidal
4 x 4
1.5 mm step in x & y
~0.563 cm2
4 x 4
1.5 mm step in x
1.0 mm step in y
~0.45 cm2
Deuterium only
Calibration factor for 20th December needed

## Slide 12: 14IWG1B Poloidal

## Slide 13: 14IWG1A

## Slide 14: 14IWG1A Poloidal
Deuterium only
4 x 4
1.5 mm step in x & y
~0.563 cm2
4 x 4
1.5 mm step in x
1.0 mm step in y
~0.45 cm2

## Slide 15: 14IWG1A Poloidal

## Slide 16: 14IWG1A Toroidal
Deuterium only
4 x 4
1.5 mm step in x
1.0 mm step in y
~0.45 cm2

## Slide 17: 14IWG1A Toroidal
Deuterium only
4 x 4
1.5 mm step in x
1.0 mm step in y
~0.45 cm2
No RGA7 data as AMU5 LOD