## Slide 1
Development of Diagnostics for Plasma-Wall Interaction in EAST and BEST
R. Yan, Y. M. Liu, L. Mu, Zhenhua Hu, Fang Ding, Xiaoyue Hu, Zhigang Cao, Baoguo Wang, J. L. Chen
Oct. 19-21, 2026. Frascati, Italy
8th International Conference on Frontiers in Diagnostics Technologies
E-mail: yanrong@ipp.ac.cn
Institute of Plasma Physics, Chinese Academy of Sciences

## Slide 2: Outlines
Introduction
Development of diagnostics for plasma wall interaction in EAST
Plasma wall interaction related diagnostics in BEST
Summary and outlook

## Slide 3
Introduction
Plasma facing materials face severe challenges:
  Extreme particle and heat flux
  Erosion of wall materials
  Impurity and confinement degradation
Plasma wall interaction (PWI) related diagnostics are important:
  Edge plasma parameters
  Change of wall conditions
  Understand plasma physics
Several PWI diagnostics have been developed in EAST and are planned in BEST.

## Slide 4: Outlines
Introduction
Development of diagnostics for plasma wall interaction in EAST
  Laser induced breakdown spectroscopy (LIBS)
  Edge spectroscopic diagnostic
  Quartz crystal microbalance (QMB)
  Low energy neutral particle analyzer (LENPA)
Plasma wall interaction related diagnostics in BEST
Summary and outlook
QMB
QMB
LIBS
LENPA

## Slide 5: Laser induced breakdown spectroscopy (LIBS)
Divertor scanning
Distance: 3 - 5 m
System Specifications
Laser：Q-SMART 850 1064 nm
Spectrometer：
Horiba iHR550+iCCD (400-780nm)
二级扩束
In situ Endoscopic coaxial LIBS system have been developed for real-time monitoring of EAST divertor wall surface conditions (retention and impurity).
Features a compact, coaxial optical design for high spatial resolution ( < 1 mm) and high spectral resolution( 0.03 nm).
Coaxial optics
Laser
Mirror
Motor stage
Mirror
Signal collection
Beam expander
Divertor
Plug in LIBS system
60cm*120cm
30cm*60cm
Robust

## Slide 6: Edge spectroscopic diagnostic
Optical transfer and detection
F. Ding et al., NME 2024
Flux of single ionsed W:
W sputtering flux from neutral W line observation
S for ioniSation rate coeffecient
X for eXciatation rate coeffecient
B for Branching ratio
Edge spectroscopic diagnostic has been developed to measure the W atom flux sputtered from the plasma facing materials.
W from divertors and first wall at high field side and Limiter at low field side has been measured.
Measured wavelength ranged from 380 – 700 nm.
2 mm
0.05 ms
0.03 nm

## Slide 7: Quartz crystal microbalance (QMB)
Al coating
8 mm
Resonance change related to mass change: ∆m=-c ∆f
Real-time monitor
High resolution of ng·cm-2
QMB can be used to monitor the material deposition and erosion which uses the piezoelectric effects of crystal material.
Au+Cr+SiO2+Cr+Au+W coating (50 nm）
Dual sensor system: Working and reference sensor
Active water‑cooling system
Data transfer and acquisition system
Nucl. Materi. Energy 38 (2024) 101576

## Slide 8: Low energy neutral particle analyzer (LENPA)
Time of flight (TOF) LENPA
Location：mid-plane in H sector
Energy range：20~3000 eV
Sampling rate：1 GS/s
Time resolution：104 μs
Neutral energy spectrum
N(E), given by LENPA
,detection efficiency
, solid angle of LENPA
LENPA has been developed to measure the neutral particle flux and energy distribution

## Slide 9: Outlines
Introduction
Development of diagnostics for plasma wall interaction in EAST
Plasma wall interaction related diagnostics in BEST
  Divertor laser induced spectroscopy (DiLIS)
  Divertor ablation monitor system (DAMS)
  Divertor dust monitor system (DDMS)
  Material probe (MP)
Summary and outlook
Upper port
DAMS
DiLIS
DAMS
DiLIS

## Slide 10: Divertor laser induced spectroscopy (DiLIS)
DiLIS 01 at upper port C(impurity composition , D/T retention, 1 s, 30 mm)
Laser injection, signal collecting
Share port plug with gas injection system and the glow discharge system
DiLIS 02 at upper port E (ne, 10 - 100 ms, 50 mm)
Signal collecting for divertor passive spectrum
Share port plug with laser induced fluorescence
Main parameters
Wavelength: 350-700 nm
Distance: ~8 m
Target size: 30 x 300 mm2
Spatial resolution: 30 mm
Fiber size: 400 μm
Main components
Spectrometer
EMCCD
ICCD, PMT
Camera
Nd: YAG laser: 1064 nm, 1.5 J, 8 ns
Layout of DiLIS
Passive spectroscopy + Laser Spectroscopy

## Slide 11: Divertor ablation monitor system (DAMS)
Laser 1
Laser 2
Upper port M
Upper port I
signal processing instrument
35 m
17.5 m
Port cell
optical system: Vacuum chamber
Front-end optical detection system: Port Cell (electromagnetic and neutron shielding)
Back-end Data Acquisition and Processing System: Outside Bio-Shielded Walls
Subsystem layout
Laser spot diameter on divertor surface ϕ= 100 mm
Depth resolution：15 μm
Lateral resolution: 10 μm
Front-end optical inspection system
Laser holography technique is used to in situ measure the surface morphology of divertor
Layout of the DAMS
Dual-wavelength digital holography technology for high-precision, wide dynamic range surface morphology measurements.
Laser wavelength: 532 nm and 530 nm
equivalent wavelength
141 μm

## Slide 12: Divertor dust monitor system (DDMS)
Piping layout: 16 vacuum suction pipes in the lower window, anti-dust tritium compatible valves.
anti-dust tritium compatible valves
branch pipes
(50 mm)
Main loop pipe (100 mm)
Dust contained gas
clean gas
Location at B1，connection with pump tube along the lower window wall.
Regularly remove and analysis the accumulated dust from bottom of the lower divertors.
Dust analysis
Dust extraction position

## Slide 13: Material probe (MP)
Measurement function
Neutral-induced material erosion
Fuel retention in first wall material
Layout of MPs
W coating + Inconel 718 substrate
Modified bolt
W erosion estimation by 3D-GAPS
MP mock-up
Test in EAST
No. | W coating | Thickness resolution | Postern measurements
＞100 | ~1 μm | ~ 1 nm | RBS, SEM, EDS, FIB etc.

## Slide 14: Outlines
Introduction
Development of diagnostics for plasma wall interaction in EAST
Plasma wall interaction related diagnostics in BEST
Summary and outlook

## Slide 15: Summary and outlook
Plasma wall interaction related diagnostics have been developed in EAST and designed in BEST.
LIBS, edge spectroscopic, QMB and LENPA have been developed to real-time monitor the divertor and first wall condition in EAST.
DiLIS, DAMS, DDMS and MP have been designed to monitor the condition of divertor, and first wall of BEST.
Wall surface topography monitoring diagnostic system will be developed next year and experiments are planned in EAST to support the development of diagnostic for BEST.

## Slide 16
Thanks for your attention！