## Slide 1: Advanced Spectroscopic Characterization Across Diverse Cultural Heritage Materials: A Synergistic Approach Using LIF, Raman, LIBS, and Multi- and Hyperspectral Imaging
Valeria Spizzichino
NUC-TECFIS-DIM (Diagnostic and Metrology Laboratory)
ENEA Frascati
ICFDT (International Conference Frontiers in Diagnotics Technologies)
October 19th 2026

## Slide 2: Why?
to:
understand culture, art history, and society
study its techniques
restore it
protect it
document and preserve a record of it
develop new ways of experiencing it
Delicate assets, unique items, and hostile environments (high-risk for the artwork and the operator, or difficult to access).
Studying a cultural asset and the environment in which it is preserved

## Slide 3: How?
Techniques distinct from standard analytical chemistry methods
(chromatography, ICP, …)
Non-sampling, non-destructive, non-invasive, non-contact, remotely operable, and rapid techniques that are independent of environmental and lighting conditions
…even if…
They may have lower sensitivity, spatial resolution, and selectivity.
One must be able to understand the needs, limitations, and advantages in order to choose the techniques to use.

## Slide 4: How?
Spectroscopic techniques
  Absorbtion methods
    Emission methods
Classified according to the spectral region involved
Notes:   Assorbimento: Radiation attenuation
    Emissione (reemitted radiation)
Raggi gamma: combiamento della configurazione nucleare
Raggi x + uv vis: cambiamento della distribuzione elettronica
IR: vibrazioni molecolari
Microonde: rotazioni molecolari
Onderadio: cambiamento dello spin

## Slide 5: How?
LIF, LIBS
Raman
(energy transition: IR … but …
(excitation: UV, VIS, NIR)
Reflectance
Notes:   Assorbimento: Radiation attenuation
    Emissione (reemitted radiation)
Raggi gamma: combiamento della configurazione nucleare
Raggi x + uv vis: cambiamento della distribuzione elettronica
IR: vibrazioni molecolari
Microonde: rotazioni molecolari
Onderadio: cambiamento dello spin

## Slide 6: LASER Spectroscopy
Light Amplification by Stimulated Emission of Radiation
Monocromaticity
Coherence
Collimation
High brilliance (high power on small areas)

## Slide 7: LASER technologies for Cultural Heritage: not only spectroscopy
Laser cleaning
Diagnostics on CH for info on CHEMICAL COMPOSITION
LIBS (Laser Induced Breakdown Spectroscopy): elementary info
LIF (Laser Induced Fluorescence): MOLECULAR + CHEMICAL SORROUNDING
Raman:
MOLECULAR + CHEMICAL SORROUNDING
Physical structure (defect localization)
• Multispectral imaging
• Interferometry, speckle interferometry
• Holography, holographic interferometry
• Laser vibrometry
Techniques for climate and microclimate evaluation
LIDAR (LIght Detection And Ranging)
Morfological techniques
• 3D scanning + time of flight methods • Triangulation scanning • Surface profilometry
• Laser scatterometry • Laser tomography (OCT)

## Slide 8: LIBS (Laser Induced Breakdown Spectroscopy)
m
Creation of a plasma on the target surface.
Evaporation of a small portion of the sample and formation of the plume. Formation of the first free electrons.
Electron bremsstrahlung results in the emission of intense continuous radiation.
Atomic emission lines are visible for a few ms.
Emissions resulting from plasma cooling cease, while surface evaporation continues, accompanied by the ejection of nanoparticles.
Finger print
Pulsed laser

## Slide 9: LIBS (Laser Induced Breakdown Spectroscopy)
Parameters that determine the characteristics of plasma:
laser wavelength
pulse duration
pulse fluence
environment or atmosphere in which the measures take place
matrix of the sample under analysis
Notes: Wavelength: Il numero di fotoni assorbiti dagli elettroni liberi presenti nella plume cresce proporzionalmente a 2
Fluence: Ad alte fluenze il calore è ceduto alla superficie troppo velocemente per essere trasferito altrove. Il calore latente di evaporazione diventa un parametro fondamentale per la determinazione della quantità di plume prodotta e delle sue caratteristiche
Atmosphere: Differenti valori di pressione e presenza di acqua o altri liquidi influenza l’evoluzione della plume
Matrix effect: Per matrici isolanti il tempo di vita media del plasma è più corto che per matrici metalliche

## Slide 10: LIBS (Laser Induced Breakdown Spectroscopy)
Quantitative analysis
Qualitative analysis
Comparison with reference database
Notes: Optically thin plasma: Gli effetti di riassorbimento sono trascurabili
LTE: processi indotti da collisioni sono di un ordine di grandezza più frequenti di quelli radiativi e valgono:
Funzione di distribuzione di Maxwell per la velocità delle particelle
Funzione di distribuzione di Boltzmann per la popolazione degli stati eccitati
Legge di azione di massa per molecole e loro prodotti di dissociazione
Legge di Saha per specie neutre e loro prodotti di ionizzazione

## Slide 11: LIBS (Laser Induced Breakdown Spectroscopy)
Quantitative analysis
Qualitative analysis
Comparison with reference database
Notes: Optically thin plasma: Gli effetti di riassorbimento sono trascurabili
LTE: processi indotti da collisioni sono di un ordine di grandezza più frequenti di quelli radiativi e valgono:
Funzione di distribuzione di Maxwell per la velocità delle particelle
Funzione di distribuzione di Boltzmann per la popolazione degli stati eccitati
Legge di azione di massa per molecole e loro prodotti di dissociazione
Legge di Saha per specie neutre e loro prodotti di ionizzazione

## Slide 12: LIBS (Laser Induced Breakdown Spectroscopy)
Quantitative analysis
Qualitative analysis
Comparison with reference database
Ca II
Notes: Optically thin plasma: Gli effetti di riassorbimento sono trascurabili
LTE: processi indotti da collisioni sono di un ordine di grandezza più frequenti di quelli radiativi e valgono:
Funzione di distribuzione di Maxwell per la velocità delle particelle
Funzione di distribuzione di Boltzmann per la popolazione degli stati eccitati
Legge di azione di massa per molecole e loro prodotti di dissociazione
Legge di Saha per specie neutre e loro prodotti di ionizzazione

## Slide 13: LIBS (Laser Induced Breakdown Spectroscopy)
Quantitative analysis
Qualitative analysis
Comparison with reference database
Al I
Notes: Optically thin plasma: Gli effetti di riassorbimento sono trascurabili
LTE: processi indotti da collisioni sono di un ordine di grandezza più frequenti di quelli radiativi e valgono:
Funzione di distribuzione di Maxwell per la velocità delle particelle
Funzione di distribuzione di Boltzmann per la popolazione degli stati eccitati
Legge di azione di massa per molecole e loro prodotti di dissociazione
Legge di Saha per specie neutre e loro prodotti di ionizzazione

## Slide 14: LIBS (Laser Induced Breakdown Spectroscopy)
Stoichiometric evaporation
Optically thin plasma
LTE (Local Thermodynamic Equilibrium)
Quantitative analysis
Qualitative analysis
IF
Comparison with reference database
Calibration Curves
Calibration free
Multivariate analysis and AI
Notes: Optically thin plasma: Gli effetti di riassorbimento sono trascurabili
LTE: processi indotti da collisioni sono di un ordine di grandezza più frequenti di quelli radiativi e valgono:
Funzione di distribuzione di Maxwell per la velocità delle particelle
Funzione di distribuzione di Boltzmann per la popolazione degli stati eccitati
Legge di azione di massa per molecole e loro prodotti di dissociazione
Legge di Saha per specie neutre e loro prodotti di ionizzazione

## Slide 15: LIBS (Laser Induced Breakdown Spectroscopy)
Database built-up: renaissance pigments a fresco
Special attention to mixtures that characterize schools and artists
“Verdaccio”
rinzaffo
arriccio
intonachino
pigment
substrate

## Slide 16: LIBS (Laser Induced Breakdown Spectroscopy)
Database built-up: renaissance pigments a fresco
Special attention to mixtures that characterize schools and artists
“Verdaccio”

## Slide 17: LIBS (Laser Induced Breakdown Spectroscopy)
Database built-up: renaissance pigments a fresco
Special attention to mixtures that characterize schools and artists
“Incarnato ”: San Giovanni white + red ocre + terra verde antica
Not just absolute intensities, but also intensity ratios for characterizing materials
Linear LIBS trend relative to the percentage of San Giovanni white

## Slide 18: LIBS (Laser Induced Breakdown Spectroscopy)
Ceramic, III-IV century b.C.
Monte Sannace (Gioia del Colle, Bari)
Local

## Slide 19: LIBS (Laser Induced Breakdown Spectroscopy)
Ceramic, III-IV century b.C.
Monte Sannace (Gioia del Colle, Bari)
Local
Elemental qualitative analysis
Stratigraphic analysis
Shot number

## Slide 20: LIF (Laser Induced Fluorescence)
The Jablonski diagram explains in detail what can happen after the absorption of a photon by a molecule, causing an electronic excitation
The fluorescence spectrum is the molecular fingerprint, as it represents the distribution of its excited and ground vibrational states.

## Slide 21: LIF (Laser Induced Fluorescence)
Energy
Fluorescence
The use of a laser allows for a more intense and simpler fluorescence spectrum

## Slide 22: LIF (Laser Induced Fluorescence)
Chemical characterizazion of materials
(chemical molecular analysis)
Molecular spectroscopy
(study and characterization of vibronic levels)

## Slide 23: LIF (Laser Induced Fluorescence)
Parameters that affect the measurement results:
Excitation wavelength
Detection temporal range
Detection wavelength
Notes: Wavelength: Il numero di fotoni assorbiti dagli elettroni liberi presenti nella plume cresce proporzionalmente a 2
Fluence: Ad alte fluenze il calore è ceduto alla superficie troppo velocemente per essere trasferito altrove. Il calore latente di evaporazione diventa un parametro fondamentale per la determinazione della quantità di plume prodotta e delle sue caratteristiche
Atmosphere: Differenti valori di pressione e presenza di acqua o altri liquidi influenza l’evoluzione della plume
Matrix effect: Per matrici isolanti il tempo di vita media del plasma è più corto che per matrici metalliche

## Slide 24: LIF (Laser Induced Fluorescence)
Parameters that affect the measurement results:
Continuous or pulsed laser
laser wavelength
pulse duration
Laser intensity  damage threshold study
Sensitivity of the detector
Time resolution
Point measurements? Imaging? Multispectral? Hyperspectral?
Notes: Wavelength: Il numero di fotoni assorbiti dagli elettroni liberi presenti nella plume cresce proporzionalmente a 2
Fluence: Ad alte fluenze il calore è ceduto alla superficie troppo velocemente per essere trasferito altrove. Il calore latente di evaporazione diventa un parametro fondamentale per la determinazione della quantità di plume prodotta e delle sue caratteristiche
Atmosphere: Differenti valori di pressione e presenza di acqua o altri liquidi influenza l’evoluzione della plume
Matrix effect: Per matrici isolanti il tempo di vita media del plasma è più corto che per matrici metalliche

## Slide 25: LIF (Laser Induced Fluorescence)
Analysis of single spectral bands
Qualitative analysis
Bands of specific molecules well known from literature
Clorofilla
Clorophyill a
(685, 740 nm)
Vitamine K,
β-carotene
(460 nm)
Riboflavin
(525 nm)
Multivariate analysis and AI
Complex spectra, convolution of many bands, large amount of data

## Slide 26: LIF (Laser Induced Fluorescence)
Same author, same production year, similar aspect

## Slide 27: LIF (Laser Induced Fluorescence)
Same author, same production year, similar aspect
505 nm
455 nm
342 nm
San Giovanni white (CaCO3)
+
titanium oxide
Gypsum (CaSO4)

## Slide 28: LIF (Laser Induced Fluorescence)
Cases in which the restoration work itself is a work of art
@ 376 nm
Dopo elaborazione
Dopo elaborazione
processed
Integration using a different type of marble (Renaissance)
Modern intervention using polymeric consolidants and whitening agents
processed

## Slide 29: LIF (Laser Induced Fluorescence)
Cases in which the restoration work itself is a work of art

## Slide 30: Raman Spectroscopy
Giving rise to this kind of spectra
A visible-light photon can be scattered by a solid lattice, a liquid, or a gas, accompanied by the emission or absorption of a phonon (a vibrational quantum).
This inelastic scattering is much less intense (because it occurs far less frequently) than elastic scattering (Rayleigh scattering)  laser source.
Notes: The molecule returns to its initial level and re-emits a photon with the same energy as the incident photon (Rayleigh scattering).
The molecule falls into a level higher than the initial one and emits a photon with a lower frequency (Stokes Raman scattering).
The molecule ends up in a state lower than the original one and emits light with a higher frequency (anti-Stokes Raman scattering).

## Slide 31: Raman Spectroscopy
Fine plaster:
CaCO3 + pozzolana
Lattice modes
bending CO32-
stretching CO32-
The presence of fluorescence bands (of much higher intensity) can be the handicap
Importance of the excitation wavelength
Large bands of amorphous materials
information on the type of molecules and the crystalline phases

## Slide 32: Raman Spectroscopy
Palazzo Chigi in Ariccia
Calcite spectrum and bands at 1436 and 1750 cm⁻¹  thin layer of vegetable oil (linseed oil, poppy seed oil)

## Slide 33: Raman Spectroscopy
Palazzo Chigi in Ariccia
225, 285, 886, 1061, 1127, 1296, 1440, 2846, 2881 cm⁻¹  beeswax
Enhancement and recognition of Raman lines with respect to fluorescence background, automatic comparison with databases

## Slide 34: LIF, LIBS, Raman Spectroscopy
LIBS, LIF, and Raman systems share a large portion of their components.
What distinguishes these systems?

## Slide 35: LIF, LIBS, Raman Spectroscopy
StellarNet
Princeton Istruments
Madrid University
Raman
LIF
LIBS

## Slide 36: LIF, LIBS, Raman Spectroscopy
Applications in the field of Cultural Heritage:
Characterization
Authentication
Dating
Restoration
Conservation
Non-destructiveness (LIF, Raman), micro-destructiveness (LIBS)
Rapidity
Sensitivity
As-is samples
In situ analysis
They are highly valued in the cultural heritage sector for:
complementarity

## Slide 37: LIF, LIBS, Raman Spectroscopy
For metals and alloys:
LIBS
For synthetic and natural organic material:
LIF + Raman
Waxes
Fabrics
Cellulose
Protective agents
Consolidants
Colorants
…
For ceramic materials and pottery:
LIBS + Raman
For inorganic pigments:
LIBS + LIF + Raman
+ colorimetry
Hyperspectral camera
XRF …

## Slide 38: In situ campaigns

## Slide 39
valeria.spizzichino@enea.it
Thanks for your attention