## Slide 1
ENR-PRD.MAG-T013 –
Progress in chemical HTS tape preparation
M. J. Wolf

## Slide 2: Task completion schedule
ENR-PRD. MAG-T013 | D001 | Report on progress in chemical HTS tape preparation | 
Technical Specification:
Monitoring of progress of HTS tapes produced by chemical methods
Investigation of HTS cable using REBCO tapes prepared by chemical methods

## Slide 3: Progress of HTS tapes
Basic understanding of chemical HTS deposition is growing (e.g. Minjuan Li et al. Coatings 2020, 10, 31; doi:10.3390/coatings10010031 Different oxygen partial pressure and heating conditions allow to optimize Jc

## Slide 4: Industry is optimizing performance (even at 5 T and 20 K, ≈ 100 A is feasible in the disadvantageous field orientation for a 4 mm wide tape )
M. Bäcker et al. EUCAS, Glasgow (1-5. Sept. 2019)

## Slide 5: Large scale 40 mm wide tape production is at hand
M. Bäcker et al. EUCAS, Glasgow (1-5. Sept. 2019)

## Slide 6: 400 m tape length is targeted
M. Bäcker et al. EUCAS, Glasgow (1-5. Sept. 2019)

## Slide 7: Slicing of 4 mm strips gives good results
M. Bäcker et al. EUCAS, Glasgow (1-5. Sept. 2019)

## Slide 8: Ni9W substrate gives more mechanical strength, optimized texture and is nonmagnetic
M. Bäcker et al. EUCAS, Glasgow (1-5. Sept. 2019)

## Slide 9: Next step: from 40 mm to 100 mm tape width will increase efficiency
M. Bäcker et al. EUCAS, Glasgow (1-5. Sept. 2019)

## Slide 10: Investigation of HTS cable using REBCO tapes prepared by chemical methods
d-nano tape of the Ni5W type was purchased with an Ic (77 K, sf) of approx. 90 K

## Slide 11: HTS CroCo - geometry
The mechanical performance of d-nano tapes is weaker than most Hastelloy-based coated conductors due to the RABITS – Ni5W – substrate of d-nano tapes.
We used copper-plated steel tapes in the HTS CroCos for mechanical reinforcement
D-nano tapes are available only in 4 mm width  change of geometry compared to CroCos of other recent projects.
  Orange: copper tape
  Green: copper-plated steel tape
  Blue: HTS tape
4 mm
3 mm

## Slide 12: HTS CroCo fabrication
Use of the new HTS CroCo fabrication setup

## Slide 13: Sample preparation of a d-nano HTS CroCo
Untwisted sample
Cross-shape of tapes very good,
Round overall shape to be optimized
Material | Width | Thickness | Length | Number
Cu | 3 mm / 4 mm | 200 µm | 4 m | 4 / 12
Steel | 3 mm / 4 mm | 87 µm | 4 m | 2 / 4
D-nano | 4 mm | 75 µm | 4 m | 2

## Slide 14: Critical Current Measurement at 77 K
Critical current of HTS CroCo as expected with two REBCO tapes, due to Ic of individual tape segments ~ 90 - 100 A
June 2019

## Slide 15: New CroCo formed with optimized outer form
Steel tape
REBCO tape
Steel tape
Steel tape
Steel tape
Steel tape
REBCO tape
Steel tape

## Slide 16: Ic of new CroCo reduced with low n-value
Problem: too high forces during CroCo manufacturing?
Recheck of an unprocessed d-nano REBCO tape

## Slide 17: Next steps in 2020
Continued analysis of degraded sample
Force monitoring during CroCo processing should be implemented
New d-nano Ni9W REBCO tapes with higher mechanical strength should be investigated (if material is available in time)

## Slide 18
Progress in chemical HTS tape preparation
Monitoring of progress of HTS tapes produced by chemical methods
Investigation of HTS cable using REBCO tapes prepared by chemical methods
Start: 01.03.2020
End: 31.10.2020
Resources: 0.1 ppy
Proposal 2020