## Slide 1
Direct Spooling of partially equipped CroCos
ENR-PRD.Extra
W.H. Fietz, M.J. Wolf, D. Nickel, K.-P. Weiss

## Slide 2: Formation of straight HTS CroCos
      From single tapes a long length straight HTS CroCo was formed with up to 60 Cu and HTS tapes in lengths up to 8 m.
      This is proofed technology and was used to build 35 kA @ 77K, sf demonstrator

## Slide 3: Bending Radius of HTS CroCos
      With respect to winding, the small 3/2 HTS CroCos from 3 mm and 2 mm tapes offer an advantageous small acceptable bending radius.
 | 6/4 CroCo | 3/2 CroCo
Typical number of REBCO tapes | 22 x 6 mm | 18 x 3 mm
 | 10 x 4 mm | 10 x 2 mm
Cross diagonal | 7.2 mm | 3.6 mm
Min. bending radius | 60 cm | 30 cm
Ic T = 77 K, self field | 3 100 A | 1 460 A
Ic T = 4 K, B = 12 T | > 10 000 A | 6 000 A
      Is it possible to spool 3/2 mm HTS CroCos directly from reel to reel to fabricate long lengths of such 3/2 HTS CroCos?

## Slide 4: Spooling of 3/2 HTS CroCos
      Due to the limited resources, existing equipment was used
      In this case, several welding positioners were tested to identify the best one for spooling the HTS CroCos

## Slide 5: Reel to Reel situation
The 1 m diameter reel
of the welding positioner
receives the HTS CroCos
prepared from the individual reels of the REBCO and Cu tapes

## Slide 6: First run of reel to reel spooling

## Slide 7: Spooling of the 3/2 HTS CroCo

## Slide 8: HTS CroCo after removal from the welding positioner
30 cm

## Slide 9: This CroCo was wound to a 60 cm diameter spool and tested. The CroCo is still superconducting after the reel-to-reel fabrication.

## Slide 10: The 3/2 HTS CroCo was straighten and re-bend several times to check degradation issues
wound in counter direction

## Slide 11: The 3/2 HTS CroCo was straighten and re-bend several times to check degradation issues
wound in counter direction

## Slide 12: 8 m HTS CroCo wound to the 1m diameter reel
In Dec 2019 approx. 8 m of HTS CroCos were fabricated –
starting from the REBCO and Cu-tape reels with subsequent winding
of the fabricated CroCo to the 1 m diameter reel.

## Slide 13
Long length fabrication and detailed analyses of CroCos towards HTS feeders for future fusion machines
Spooling of long length partially equipped CroCos
Preparation of 8 m fully equipped TS CroCos
Intensive examination of fully equipped CroCos
Start: 01.03.2020
End: 31.10.2020
Resources: 2.0 ppy
Proposal 2020