## Slide 1
MAG-5.3-T016 -
Development of High Current HTS cables
M. J. Wolf

## Slide 2: Task completion schedule
MAG-5.3-T016 | D001 | Development of High Current HTS cables | 
Technical Specification:
• Design of HTS CroCo winding demonstrator - postponed to 2020 or later
• Adaptation of HTS CroCo samples towards a winding demonstrator - ongoing (focused)

## Slide 3: Proposed modification of the „long-term agenda“
Integration of the following intermediate step:
Detailed Investigation of straight HTS CroCo triplet samples

## Slide 4: Determination of the friction factor of triplet samples
So far, we used the friction factor correlation of the EURATOM LCT coil in the thermohydraulic calculations of HTS CroCo-based conductors, e.g. tripletts samples.
This should be checked by dedicated experiments.
Three samples with different strand diameters and copper profiles were prepared and shipped to Monika Lewandowska for testing.

## Slide 5: Preparation of triplet samples
Three soft-annealed copper rods of 6.0 and 8.0 mm diameter served as HTS CroCo dummy conductor and were manually twisted.
The twisted triplet samples were inserted into a stainless-steel tube and compacted to touch the twisted triplet.
Sample (steel tube) length ~ 1.3 m

## Slide 6: Preparation of triplet samples with Cu-profiles
Three copper profiles were equipped with (dummy) HTS CroCos by soldering them to the profiles with In50Sn50 solder.
The triplet was manually twisted (TP = 40 cm).
The twisted triplet samples were inserted into a stainless-steel tube and compacted to touch the twisted triplet.
Sample length: 1.0 m
Pressure drop measurements to be performed in 2020 ( TS proposal for 2020 by M. Lewandowska)

## Slide 7: Test results of sample 1&2 (by M. Lewandowska)
M. Lewandowska, et al., “Hydraulic characterization of conductor prototypes for fusion magnets” presented at CHATS-AS 9-12 July 2019, Szczecin, Poland, online: https://indico.cern.ch/event/776034/contributions/3445045/attachments/1878471/3094079/ML_CHATS-AS-2019_hydraulic.pdf

## Slide 8: Preparation of HTS CroCo samples for electromechanical testing
For details, refer to the (following) presentation by K.-P. Weiss:
Material | Width | Thickness | Length | Number | Ic (77K, sf) min/max
Cu | 3 mm / 2 mm | 200 µm | 8 m | 5 / 2 | -
HTS tape | 3 mm / 2 mm | ~ 90 µm | 8 m | 10 / 4 | 90 - 118 / 60 – 80

## Slide 9
Summary
Preparation of three samples for pressure drop testing
Preparation of HTS CroCo samples for further electro-mechanical testing

## Slide 10
Development of High Current HTS cables
Preparation of HTS CroCo triplet samples, profile mockup-preparation for further testing (AMT 5.5, K.-P. Weiss)
Start: 01.03.2020
End: 31.10.2020
Resources: 0.1 ppy
Proposal 2020