## Slide 1: MAG-5.3: HTS conductor design and development
Ortensia Dicuonzo
Davide Uglietti

## Slide 2: Task specification 2019
FEM: understand the stress components in the stack under transverse compression and identify which type of reinforcement should be used to limit the strand deformation.
Testing various types of reinforcement on dummy strands.
Preparation and test of sub-size samples for a new cable concept: the stacks are directly cabled and soldered around a flat core and soldered to the jacket (solder filled or monolithic conductor).
In summer 2019 selection of two designs.
Conductor preparation in the second half of 2019.

## Slide 3: 1. Mechanical model features
2D Generalized plain strain, free endings;
Force 0-115 kN·m (80 kN·m max force in the cable);
Cool down RT-77K thermal expansion coefficient of the materials;
Symmetric wrt to the xz and yz plane;
Plastic (Bilinear), yield strength(T);
90o and 45o.
Force
Solder
Copper
Wire
Anvil
Delamination tension ()
Pretension in the wire
F
Stack
Reinforced soldered TSTC in round shells

## Slide 4: 1. Results
(*)
(*)
(*)
Big improvement can be obtained by using aluminum alloy 7075-T7 and reducing the copper cross section.
The solutions proposed are not helpful wrt the shear stress at 45o;
The delamination at 45o can be eliminated by using alloy 7075-T7.
Reference case
Annealed copper;
7 mm Φ
(*) H. Maeda et al., DOI:10.1109/TASC.2013.2287707
Tape mechanical properties, Nathaniel C. Allen et al., DOI: 10.1109/TASC.2017.2652304
Unfortunately, it was not possible to find the aluminium alloy 7075 in wire form and this design option was abandoned.

## Slide 5: Task specification 2019
FEM: understand the stress components in the stack under transverse compression and identify which type of reinforcement should be used to limit the strand deformation.
Testing various types of reinforcement on dummy strands.
Preparation and test of sub-size samples for a new cable concept: the stacks are directly cabled and soldered around a flat core and soldered to the jacket (solder filled or monolithic conductor).
In summer 2019 selection of two designs.
Conductor preparation in the second half of 2019.

## Slide 6: 2. Sample description
Indium tape across the stack to increase the contact between tapes and copper.
Two copper tapes: ↑the compactness of the stack ↓ the intertape resistance.
Stainless steel wire diameter (AISI 304), 0.5 mm
Annealed copper shells, Φ 7 mm
Features of the sample | 
Tape | SST tape, 3.3 mm width
Number of tapes | 28
The strand is twisted and then wrapped with stainless steel wire at constant tension of 30 N.
The tested regions belong to the same sample.
Not-soldered TSTC in round shells

## Slide 7: 2. Experimental set-up and Results
The transverse force at which the irreversibility is reached Flim < Fcable … this strand cannot be used for the Rutherford cable.
No difference among the different directions.
Large scattering in Ic … because of the varying inter-tape resistance.
The plastic deformation of the copper shells diameter is high: ~10% ( 1 mm)!
77 K, s.f., 4 points method
F0o
F45o
F90o

## Slide 8: Task specification 2019
FEM: understand the stress components in the stack under transverse compression and identify which type of reinforcement should be used to limit the strand deformation.
Testing various types of reinforcement on dummy strands.
Preparation and test of sub-size samples for a new cable concept: the stacks are directly cabled and soldered around a flat core and soldered to the jacket (solder filled or monolithic conductor).
In summer 2019 selection of two designs.
Conductor preparation in the second half of 2019.

## Slide 9: 3. Sample preparation
Features of the sample | 
Tape | SST tape, 3.3 mm width
Tapes/stack | 10
Cabling angle | 10o
Core thickness | 6 mm
The most critical part under transverse pressure is where the tapes are bent!
One stack of tapes cabled around the copper core…
The sample is placed inside a stainless steel jacket…
and filled by
Sn60Pb40 solder.
No tensile strain during cabling;
Solder filled after cabling;
the stacks are fixed in place;
the solder filling should ensure hydrostatic distribution of transverse pressure;
high thermal conductivity between cable and jacket.
Cable twist pitch: ~600mm.

## Slide 10: 3. Experimental set-up and Results
F
F
w
Stack
Copper core
Jacket
Solder
The regions belong to the same sample;
Length of the anvil, l=30 mm.

## Slide 11: Selected designs
6 around 1
10 mm hard copper shells
40 SST 4.8 mm wide tapes per strand
5-6 mm core thickness
~45 mm wide (flat part)
~28-30 stacks
~10-12 SST 3.3 mm wide tapes per stack
Rated for 53 kA at 18T
Strand was tested successfully last year

## Slide 12: Task specification 2019
FEM: understand the stress components in the stack under transverse compression and identify which type of reinforcement should be used to limit the strand deformation.
Testing various types of reinforcement on dummy strands.
Preparation and test of sub-size samples for a new cable concept: the stacks are directly cabled and soldered around a flat core and soldered to the jacket (solder filled or monolithic conductor).
In summer 2019 selection of two designs.
Conductor preparation in the second half of 2019.

## Slide 13: 5. Conductor preparation
Done:
Copper shells and core procured;
Copper shells pre-tinned;
Tapes procured and pre-tinned.
New online soldering procedure
Done:
Tapes procured and pre-tinned;
Core procured.
Mock-up in construction;

## Slide 14: 2020
To finish the task for 2019:
  Finalization of the drawings for the cable and for the terminations;
  Jacket procurement;
  Cable assembly;
  Conductor assembly.