## Slide 1: MAG EU-CN collaboration 2019-2020
Andrea Augieri
ENEA, Frascati Research Centre - Superconductivity Laboratory
Final meeting – ENEA, February 11th 2020
ENEA HTS Cable-in-Conduit Conductor Sample

## Slide 2: ENEA HTS cable – layout
Stack configuration 20 tapes per stack
Expected cable Ic @ 12 T, 4.2 K: 250 × # tapes = 12 – 15 kA
Empty slots : for tape voltage and temperature sensors wiring
Stack distribution: alternate HTS
Twisted 6 slot Al-core (t.p. = 500 mm)
3 HTS stacks + 3 empty slots (no tapes)
HTS tape from SuperOx (4 mm x 0.15 mm)
Expected average Ic(4.2 K, 12 T) = 200-250 A

## Slide 3: ENEA HTS cable – layout: jacket
Round jacket Al-foil 1.5 mm welded and compacted by drawing
+
SS-tube (1 mm thick) crimped on Al-jacket
SS tube is functional for the cooling purpose:
guarantee suitable He-tight for the cooling system

## Slide 4: ENEA HTS cable – layout: termination
Tig-welded joint
SS tube external jacket
Cu cylinder
He inlet
Tig-welded joint
Terminator:
Cu cylinder
+
SS extremity
SS
Bottom box based on the same concept
No damage occurred on HTS tape after welding.
Successfully tested!

## Slide 5: ENEA HTS cable – layout: termination
LN2 bath Test @ ENEA 20 kA facility
Ic = 4.2 kA - cable with 2 stacks: 2 x 20 tapes
Basic features:
electrodeposited Cu coating of slots;
staggered stack end inserted into the slot of the Al-core;
triangle-shaped Cu filler
soldered with Pb-Sn paste
Cu-SS cylinder crimped on
Rterm ~ 130 nΩ

## Slide 6: ENEA HTS cable – mock-up sample
Prototype cable fro SULTAN quench experiment has been manufactured
2 m long – 3 HTS slots (20x3 tapes)
He leak test done: PASSED!
Electrical test: on going (in few weeks)
Manufacturing Photo Story
Slots Cu electro-deposition
Stack insertion
Wrapping + jacketing
Stack staggering
Cu filler insertion and soldering
Termination soldering and crimping
Several problems encountered
Several solutions found
Thanks to Marcello Marchetti
STEPS

## Slide 7: ENEA HTS cable – mock-up sample
Slots Cu electro-deposition
termination region
Cu only inside the slots
Stack insertion
1st stack

## Slide 8: ENEA HTS cable – mock-up sample
Stack insertion
2nd stack
3rd stack
Voltage taps on each stack insulated with Kapton
Wires running out from the closest empty slot

## Slide 9: ENEA HTS cable – mock-up sample
15 cm
30 cm
4 voltage taps on each stack
in the central region of the cable
More than 4 voltage taps can be placed using thinner wires

## Slide 10: ENEA HTS cable – mock-up sample
Wrapping + jacketing
Al foil
1.5 mm Al jacket
(drawing)
1.0 mm SS jacket
(no crimping)

## Slide 11: ENEA HTS cable – mock-up sample
Stack staggering
Stack staggered in 1 cm steps
Al and SS jacket removed from the termination region
Cu filler pre-shaped in the core slots

## Slide 12: ENEA HTS cable – mock-up sample
Cu filler insertion and soldering
Termination region after soldering e polishing

## Slide 13: ENEA HTS cable – mock-up sample
Cu
SS
Termination soldering and crimping
wires
Term A: In-foil
Term B: coated

## Slide 14: ENEA HTS cable – mock-up sample
Termination soldering and crimping
filled with stycast epoxy
TIG soldered
CABLE READY

## Slide 15: ENEA HTS cable – mock-up sample
We are currently manufacturing the termination plates (Cu)
ELECTRICAL TEST AT LN2 SCHEDULED FOR THE END OF FEBRUARY
The same design, with two holes, will be used in the SULTAN sample as bottom connection

## Slide 16: ENEA HTS cable – SULTAN Quench Experiment
Thank you for your
Thanks to all the ENEA HTS Cable Team and especially to M. Marchetti