## Slide 1: MAG-4.2-T011-D002 Test of R&W Prototype Joint
WPMAG Final Meeting 2019
V. D’Auria, B. Stepanov, K. Sedlak, P. Bruzzone

## Slide 2: Outline
Background of RW2 joint
RW2 joint using diffusion-bonding technique (RW2J2)
  Assembly
    Cables preparation before bonding
    Diffusion bonding
    SULTAN sample
  Test results
    Electrical resistance
    AC losses ꓕ and ‖ to the broad side
  Conclusions and perspectives

## Slide 3: Background of RW2 Joint
In 2017 failed test of a butt-joint with superconducting bridges (RW2J1). Resistance 3-13 nΩ at 0-11 T

## Slide 4: RW2J2
Inter-layer joint for React&Wind cables  joint during winding
Overlap geometry
Target R≤1 nΩ at operating conditions, B=8 T and I=63.3 kA
Diffusion bonding joint (N.B. cables already heat treated)  no solder, no flux agents, no indium wires.
Techniques/tools compatible with in situ assembly, including:
  Copper spraying method to flatten the surfaces
  Clamp to keep pressure, ≈30 MPa
  Oven to keep temperature, ≈650 °C

## Slide 5: Outline
Background of RW2 joint
RW2 joint using diffusion-bonding technique (RW2J2)
  Assembly
    Cables preparation before bonding
    Diffusion bonding
    SULTAN sample
  Test results
    Electrical resistance
    AC losses ꓕ and ‖ to the broad side
  Conclusions and perspectives

## Slide 6: RW2J2 – 1. Thermal copper spray
Aluminum clamps & bars as support
Sandblasting & copper-spray in multistage
Surfaces milled flat

## Slide 7: Outline
Background of RW2 joint
RW2 joint using diffusion-bonding technique (RW2J2)
  Assembly
    Cables preparation before bonding
    Diffusion bonding
    SULTAN sample
  Test results
    Electrical resistance
    AC losses ꓕ and ‖ to the broad side
  Conclusions and perspectives

## Slide 8: RW2J2 – 2. Clamp
Target joint pressure @ 650 °C is 30 MPa
Clamp design criteria:
  Disassembly after diffusion-bonding
  Joint pressure homogeneity
  Choice of materials such that p=24 MPa @ 20 °C  p=30 MPa @ 650 °C
Materials:
Inconel 600
Stainless steel
Glass-fiber
Cable
Displacement amplification factor=50
Notes: α_Inconel600=15.5e-6 K-1 average between 20 and 650 degrees
α_AISI304=17.5e-6 K-1 average between 20 and 650 degrees
α_AISI316=18.5e-6 K-1 average between 20 and 650 degrees
α_cable=16.5e-6 K-1 average between 20 and 650 degrees

## Slide 9: RW2J2 – 3. Oven to keep temperature (I)
Portable inductive copper oven
Ferrite blocks focus field lines
Inductors optimized  cable temperature as homogeneous as possible
Normalized
Ohmic Losses
f=52.3 kHz
P=4.6 kW
Clamp center
Clamp end
Notes: δ: penetration depth [m]
ρ: resistivity [Ωm]
μ: magnetic permeability [H/m]
f: frequency [Hz}
It shouldn’t be higher than 1/8 diameter of work piece. δ=2.2 mm for Inconel 600
𝛿=√(𝜌/(𝜋∙𝜇∙𝑓))
δ: penetration depth [m]
ρ: resistivity [Ωm]
μ: magnetic permeability [H/m]
f: frequency [Hz}
It shouldn’t be higher than 1/8 diameter of work piece. δ=2.2 mm for Inconel 600

## Slide 10: RW2J2 – 3. Oven to keep temperature (II)
(a)
Cu Inductors
Cu cooling plates
Pressure clamp
N2 inlet
(c)
Ceramic wool
N2 dewar
(b)
Mica plates
f=52.3 kHz, P=4.6 kW
Oven and cable ends active cooling
Mica plates shield from thermal radiation.
Inert atmosphere with N2
Cable T @ steady-state (P=4.6 kW, f=52.3 kHz):
  690 °C @ cable center
  620 °C @ cable ends
  20 °C @ Cu plates
Times:
  1.5 h to get steady-state
  2 h of diffusion-bonding
  6 h cool-down

## Slide 11: Outline
Background of RW2 joint
RW2 joint using diffusion-bonding technique (RW2J2)
  Assembly
    Cables preparation before bonding
    Diffusion bonding
    SULTAN sample
  Test results
    Electrical resistance
    AC losses ꓕ and ‖ to the broad side
  Conclusions and perspectives

## Slide 12: RW2J2 – SULTAN sample
  Stabilizer is machined according to joint dimensions
  Copper bridge with indium ensures full matrix stabilizer electrical continuity
  Cable preload with thin steel foil between jacket and stabilizer
  Steel end caps and bars are welded to the jacket
RRR=70
Cu bridge
Jacket
Stabilizer
joint
Dummy
joint

## Slide 13: Outline
Background of RW2 joint
RW2 joint using diffusion-bonding technique (RW2J2)
  Assembly
    Cables preparation before bonding
    Diffusion bonding
    SULTAN sample
  Test results
    Electrical resistance
    AC losses ꓕ and ‖ to the broad side
  Conclusions and perspectives

## Slide 14: Test results – Electrical Resistance
R(B) behavior according to Cu magneto-resistance for the “initial” curve
Higher difference between R450mm and R600mm after cycling (8Tx63.3kA=506 kN/m). We suspect damage @ joint sides
I=63.3 kA
Joint in TF
Stabilizer
V-taps arrays at 450 mm and 600 mm. R @ different I-flat-top and B
Notes: Joint works at 8 T, but it is important also test at 10.9 T because we use two high-grade
We suspect damage because of difference between R450 and R600 (not shown). Also because @ low fields, far from strands saturation, the average R after cycling is lower than the “initial” curve

## Slide 15: Outline
Background of RW2 joint
RW2 joint using diffusion-bonding technique (RW2J2)
  Assembly
    Cables preparation before bonding
    Diffusion bonding
    SULTAN sample
  Test results
    Electrical resistance
    AC losses ꓕ and ‖ to the broad side
  Conclusions and perspectives

## Slide 16: Test results – AC losses and Transient Stability Test
Comparison between joint and conductor at B=2 ± 0.3 T sinusoidal pulse
AC field ꓕ broad face
  No screening @ lower f  joint AC losses ≈ twice as conductor ones
  Screening @ higher f  joint and conductor losses are similar
AC field ‖ broad face: new current loops make comparison with conductor not scalable
Transient stability test at B=8 T, I=63.3 kA  quench in conductor leg if dB/dt>17.6 T/s in 128 ms. Deposited energy in joint 65 J
ΔBꓕ
ΔB‖
ΔB‖
ΔBꓕ
ΔB‖
ΔBꓕ

## Slide 17: Conclusions and perspectives
MAG-4.2-T011-D002 completed
We have a joint reference for layer-wound DEMO RW magnets
Further R&D
Further characterization of the joint
  Mechanical tests with KIT (TS for KIT)
  Micrographs to study joint uniformity
The mechanical design of the joint (jacket, stabilizer, fillers) can be improved
A new joint may be prepared using RW3 late next year
Notes: Joint costs:
Spray ≈350 CHF/cable
Inductors ≈1500 CHF
AC power supply rent ≈1200 CHF/week

## Slide 18: Backup

## Slide 19
Measuring RRR sprayed copper

## Slide 20
Diffusion bonding temperature distribution