## Slide 1: The superconducting magnet system of the Italian Divertor Tokamak Test (DTT) Facility
Luigi Muzzi
on behalf of the DTT Magnet System design team:
A. Di Zenobio, S. Turtù, L. Affinito, A. Anemona, V. Corato, C. Fiamozzi Zignani, L. Giannini, G. Messina, L. Morici, R. Righetti, G. Romanelli, L. Zoboli and A. della Corte – ENEA
R. Bonifetto, A. Zappatore and R. Zanino – Politecnico di Torino (NEMO Group)
and DTT design contributors:
see Divertor Tokamak Test facility – Interim Design Report; ed. by R. Martone, R. Albanese, F. Crisanti, P. Martin and A. Pizzuto; ISBN: 978-88-8286-378-4

## Slide 2: EU Research Roadmap to Fusion Energy
L. Muzzi - The DTT Magnet System
(Sept. 2018)

## Slide 3: DTT: Divertor Tokamak Test Facility project
General objective: create a research infrastructure addressed to the solution of the power exhaust issues in view of DEMO.
Test Divertor alternative solutions & improve experimental knowledge in the PEX scientific area
Replace Divertor by Remote Handling
High Magnetic System flexibility to Implement Various Plasma configurations
L. Muzzi - The DTT Magnet System

## Slide 4: DTT Facility Overview
L. Muzzi - The DTT Magnet System
Magnetic configurations and e.m. analysis by R. Ambrosino
The facility will offer high flexibility to test the candidate divertor concepts and to probe different magnetic (i.e. plasma) topologies

## Slide 5: Reference machine parameters
L. Muzzi - The DTT Magnet System
Max. plasma current: 5.5 MA. Inductive operation with a max. high b flat top up to 50 s.
Heating system providing 45 MW (target) (20-30 MW ECRH, 3-9 MW ICRH, 7-15 MW NNBI).
R (m) / a(m) | 2.14/0.65 SN – 2.14/0.65 DN
A | 3.3 SN/DN
Vol (m3) | ≈28
Ip (MA) | 5.5
BT (T) | 6 @ R0
Neutron production rate, Sn (n/s) | 1.2-1.5 10^17 DD + 1% DT
Maximum dwell time for high performance | 3600
Nominal repetition time after disruption (s) | 3600
Number of shots per day | 5-10
Days of operation per year | 100
Years of operation | 25

## Slide 6: DTT s.c. Magnet System Overview
L. Muzzi - The DTT Magnet System
  18 TF coils:
  Nb3Sn CICC: 42.5 kA – 11.9 T
  providing 6.0 T over plasma major radius (2.14 m)
  6 CS modules (indipendently fed)
  Nb3Sn CICC: 30 kA – 13.4 T
  providing 16.3 Weber magnetic flux for plasma initiation at breakdown
  6 PF coils
  Nb3Sn (PF1 & PF6) CICC: 28.3 kA – 8.5 T
  NbTi (PF2 to PF5) CICC: 28.6 kA – 5.4 T
  Identical in pairs to guarantee full top/down symmetry
5.3 m
2.14 m

## Slide 7: S.C. components design rationale
L. Muzzi - The DTT Magnet System
DTT superconducting coils (in terms of strands, conductor, coil winding technology) design is based on the assumption of:
tight time and budget constrains: state-of-art magnet technology choices (or close to), in order to minimize R&D.
Steel
jacket
Empty fraction for forced He circulation
1000  5000
filaments
strand
Pressure relief channel
Strand bundle
ITER TF CICC

## Slide 8: S.C. components design rationale: STRANDS
L. Muzzi - The DTT Magnet System
Courtesy A. Devred
Ic achieved: 190 A – 315 A
on 0.82 mm wire
(Vostner - SUST 2017)
Ic achieved: 325 A
on 0.73 mm wire @ 6.4 T
(Karasev – IEEE TAS 16)
Ic achieved > 260 A
on 0.82 mm wire
(Devred - SUST 2014)
all 0.82 mm wires | Min. Critical Current
DTT TF specs (Nb3Sn) | 285 A (4.2 K; 12 T; 0% strain)
DTT CS & PF1/6 specs (Nb3Sn) | 260 A (4.2 K; 12 T; 0% strain)
DTT PF2-5 specs (NbTi) | 500 A (4.2 K; 5 T)

## Slide 9: S.C. components design rationale: STRANDS
all 0.82 mm wires | Min. Critical Current
DTT TF specs (Nb3Sn) | 285 A (4.2 K; 12 T; 0% strain)
DTT CS & PF1/6 specs (Nb3Sn) | 260 A (4.2 K; 12 T; 0% strain)
DTT PF2-5 specs (NbTi) | 500 A (4.2 K; 5 T)
55 tons
22 tons
L. Muzzi - The DTT Magnet System

## Slide 10: S.C. components design rationale: STRANDS
- Nb3Sn performance depends (strongly) on strain state and sensitivity is hard to predict;
- Nb3Sn wire inside Cable-in-Conduit conductors (CICC) is subject to strain:
Breschi_SUST 2017
Typical operating range
L. Muzzi - The DTT Magnet System

## Slide 11: S.C. components design rationale: CICC
DTT CICC design is based on the results collected within a number of programs:
Present reference CICC solution based on:
rectangular geometry, with constant thickness steel jacket;
EITHER very short twist pitch cable configuration (ITER CS-like) OR long twist pitch & low Void Fraction (HFML / NHMFL-like)
Assumption: eeff = - 0.65%
Design verification with dedicated experimental tests (DC properties with e.m. and thermal cycling + AC losses) is necessary, in order to assess the actual performance.
JT-60SA
HFML
EU-Alt TF
NAFASSY
L. Muzzi - The DTT Magnet System

## Slide 12: Toroidal Field Coils
L. Muzzi - The DTT Magnet System
- CICC operating current: 42.5 KA
- Bpeak: 11.9 T
- Double pancake-winding: 3 rDP; 2 sDP; 84 turns
- Max. hydraulic length: 110 m
- Cable: 420 / 180 S.c./Cu wires
- DTmargin > 1.4 K
- Jacket: 1.9 mm 316 LN
- Turn insulation: Fiber-glass + resin
- Wind  React  Insulation  Impregnation
Overall TF energy: 2 GJ
L (1 TF coil): 48 mH
Max. Volt. at discharge < 1 kV (terminal to terminal)
TF coil height ≈ 6 m
TF coil width ≈ 3.2 m

## Slide 13: Toroidal Field Coils: analyses
2D detailed
Thermal-Hydraulics
3D global
3D submodeling

## Slide 14: Central Solenoid modules
L. Muzzi - The DTT Magnet System
5.3 m
1,5 m
Design choices:
6 identical but independent modules
Layer wound (optimized JE --> Flux > 16.3 W
Optimized concepts for inter-grade joints and terminations
High Field Section
648 s.c. wires
4.1mm jacket
Low Field Section
180 s.c. wires
2.0mm jacket
G-10 inter-module spacer (60 mm)

## Slide 15: Central Solenoid - analyses
[ Pa ]
Shear XY
3D global
2D detailed
3D submodeling
Stress level in SS is below the allowable limits for both components: membrane (667 MPa) and membrane + bending (867 MPa)
SINT
CSU1(Ur)
[ m ]
«Deformed shape x100»
CS Gravity support
(only on lower side; attached to TF casing)

## Slide 16: CS and PF support structures
CS Gravity support
(only on lower side; attached to TF casing)
L. Muzzi - The DTT Magnet System

## Slide 17: Poloidal Field Coils
L. Muzzi - The DTT Magnet System
PF1
PF2
PF3
PF4
PF5
PF6
COIL | PF1/6 | PF2/5 | PF3/4
Bmax (T) | 8.5 | 4.4 | 5.4
# turns (radial x vertical) | 20 x 18 | 10 x 16 | 14 x 14
Iop max (kA) | 28.3 | 27.1 | 28.6
ΔTmargin (Top: 4.5K) | 1.8 | 1.8 | 1.7
Hydraulic length (m) | 178 | 193 | 381
L (H) | 0.454 | 0.298 | 0.690
Vmax (V) | 2150 | 1350 | 3290
Weight (ton) | 15 | 16 | 28
Delay / discharge const. | 1.5 s / 6 s |  | 
CICC dimensions (mm) | 23.4 x 28.3 | 26.4 x 27.7 | 26.4 x 27.7
Jacket thickness (mm) | 3.0 | 3.0 | 3.0
Central channel (in/out) | 5 / 7 mm | 5 / 7 mm | 5 / 7 mm
# SC / Cu strands; 0.82 mm | 180 (Nb3Sn) / 216 | 162 (NbTi) / 324 | 324 (NbTi) / 162
PF Double or Quadri-pancake winding and joint (praying or shaking hands) boxes
DP winding for PF2 to 5

## Slide 18: Poloidal Field Coils - analyses
3D global
Fatigue assessment
Thermal-Hydraulics
Inter-pancake
Inter-turn
counter-current He flow in adjacent pancakes
common He inlet for each DP at coil bore
Target ∆Tmargin > 1.7K
is reached in each coil (AC losses values still to be experimentally verified)
L. Muzzi - The DTT Magnet System

## Slide 19: CS HTS Insert Coil
DTT as a test-bed for next generation fusion magnets
Pre-compression structures
Coil centering systems
LTS
HTS
Design of a HTS insert
(presently outside of the DTT scope)
Technical merits:
Higher Magnetic Flux (16.4 Volt sec  17.3 Volt sec)
Higher Magnetic Field (14 T  17.5 T)
Fundamental technology demonstration toward high-magnetic field fusion.

## Slide 20: CS HTS Insert Coil
L. Muzzi - The DTT Magnet System
Most recent concept
External high-strength Aluminum-alloy jacket.
L = 36 mm
6 slots for twisted stack of s.c. tapes
30 – 35 kA current in 18 T – 20 T field (to be tested)
ENEA-TRATOS Aluminum slotted Core HTS CICC

## Slide 21: Summary and perspective
  The DTT – Divertor Tokamak Test Facility is going to be built in Frascati (Italy), aimed to the study of power exhaust solutions in view of DEMO.
  The project has undergone a number of Design Review milestones, and the superconducting magnet design is being finalized. Its design was based as much as possible on already assessed technologies. All coils will be cold tested.
  First procurement milestone was the Tender for the strand supply, to be followed within the next few months by conductor and TF coil procurement tenders.
  Currently outside the scope of the project, a feasibility study is on-going, of a HTS coil to be inserted (at a later stage!) into the Central Solenoid to increase the available flux and to use DTT also as a test-bed for the development of the next generation fusion magnets.
Interim Design Report
April 2019
Ed. by R. Martone (CREATE), R. Albanese (CREATE), F. Crisanti (ENEA), P. Martin (RFX) and A. Pizzuto (ENEA)
L. Muzzi - The DTT Magnet System