## Slide 1
Measuring the equation of state of fusion-relevant foams
R.W. Paddock*, M.W. von der Leyen, R. Aboushelbaya, D.J. Chapman, D.E. Eakins,
M. Oliver, R. J. Clarke, M. Notley, C. D. Baird,
N. Booth, C. Spindloe, D. Haddock, S. Irving,
R.H.H. Scott, J. Pasley, M. Cipriani, F. Consoli,
B. Albertazzi, M. Koenig, A. S. Martynenko,
L. Wegert, P. Neumayer, P. Tchórz, P. Raczka,
P. Mabey, W. Garbett, R.M.N. Goshadze,
V.V. Karasiev, S.X. Hu and P.A. Norreys
*robert.paddock@physics.ox.ac.uk
© Crown Owned Copyright/AWE [2022]

## Slide 2
Foams and ICF
Foams are of interest for a number of reasons, including: laser beam smoothing and imprint mitigation, adiabat shaping, increasing absorption of Nd-laser light, and increasing conversion from laser light into X-rays.
They are also used in wetted foam ICF capsules, where they can be used to control convergence ratio.
We have performed 1D simulations of such capsules in an expected low-instability regime, achieving gains of 0.2 at 800kJ, and 0.8 at 1.8MJ.
References: Paddock, R. W., et al. (2021) Phil Trans R Soc A., 379(2189), 20200224
Paddock, R. W., et al. (2022) J. Plasma Phys, 88, 905880314

## Slide 3
Low instability direct-drive ICF
DT wetted foam
Total density = 253 mg/cm3
Foam only density = ~25 mg/cm3
Dry foam
Total density = Foam density =
253 mg/cm3
Laser Energy = 770 kJ, Gain = 0.2
CR = 16, Implosion Velocity = 400 km/s,
IFAR = 30
Laser Energy = 780 kJ, Gain = 0.02
CR = 16, Implosion Velocity = 390 km/s,
IFAR = 29
References: Paddock, R. W., et al. (2021) Phil Trans R Soc A., 379(2189), 20200224
Paddock, R. W., et al. (2022) J. Plasma Phys, 88, 905880314

## Slide 4
Foam equation of state
The equation of state of such foams – both in wetted foam designs, and in our hydrodynamic equivalent design – are not well characterised.
Foams are of major interest for fusion, and this limits the accuracy of simulations including them.
We performed an experiment in Jan/Feb 2022 to measure the EOS of TMPTA plastic foam using the CLF’s Vulcan laser.

## Slide 5
EOS theory
The EOS is the phase space of accessible pressure-density points to a material, and is required to close the hydrodynamic equations.
The ‘principle hugoniot’ are the pressure-density states accessible when a material is shocked.
Can consider Pressure-Density, or Shock Velocity-Particle Velocity.
Density, ρ
Pressure, P
Reference: Forbes, J.W. (2012) Shock Wave Compression of Condensed Matter. Heidelberg: Springer International Publishing

## Slide 6
Reference materials and impedance matching
Material 1 - Quartz
Reference material – EOS well known.
Measure shock velocity,
Material 2 - Foam
Material being studied – EOS unknown.
Measure shock velocity,
Shock
Shocked quartz
Unshocked quartz
Unshocked foam
Shock
Shocked quartz
Relaxed quartz
Shocked foam
Rarefaction wave
Unshocked foam
Reference: Forbes, J.W. (2012) Shock Wave Compression of Condensed Matter. Heidelberg: Springer International Publishing

## Slide 7
Reference materials and impedance matching
Particle velocity, u
Pressure, P
1
Known Quartz EOS
Reference: Forbes, J.W. (2012) Shock Wave Compression of Condensed Matter. Heidelberg: Springer International Publishing

## Slide 8
Reference materials and impedance matching
Particle velocity, u
Pressure, P
1
2
Known Quartz EOS
Quartz Rayleigh line (gradient = )
Reference: Forbes, J.W. (2012) Shock Wave Compression of Condensed Matter. Heidelberg: Springer International Publishing

## Slide 9
Reference materials and impedance matching
Particle velocity, u
Pressure, P
1
2
3
Known Quartz EOS
Quartz Rayleigh line (gradient = )
Shocked Quartz state
Reference: Forbes, J.W. (2012) Shock Wave Compression of Condensed Matter. Heidelberg: Springer International Publishing

## Slide 10
Reference materials and impedance matching
Particle velocity, u
Pressure, P
1
2
3
Known Quartz EOS
Quartz Rayleigh line (gradient = )
Shocked Quartz state
Known Quartz Release curve
Reference: Forbes, J.W. (2012) Shock Wave Compression of Condensed Matter. Heidelberg: Springer International Publishing
4

## Slide 11
Reference materials and impedance matching
Particle velocity, u
Pressure, P
1
2
3
4
Known Quartz EOS
Quartz Rayleigh line (gradient = )
Shocked Quartz state
Known Quartz Release curve
Foam Rayleigh curve (gradient = )
Reference: Forbes, J.W. (2012) Shock Wave Compression of Condensed Matter. Heidelberg: Springer International Publishing
5

## Slide 12
Reference materials and impedance matching
Particle velocity, u
Pressure, P
1
2
3
6
4
5
Known Quartz EOS
Quartz Rayleigh line (gradient = )
Shocked Quartz state
Known Quartz Release curve
Foam Rayleigh curve (gradient = )
Shocked Foam state
Reference: Forbes, J.W. (2012) Shock Wave Compression of Condensed Matter. Heidelberg: Springer International Publishing

## Slide 13
Target design
400 um
Vulcan beam
Imaged region
400 um
Side view (not to scale)
CH ablator (40 µm thick)
Gold (3 µm)
Quartz (40 µm)
Foam (40 µm)
Quartz
2 mm
2 mm
Foam
(1 mm diameter)
Imaged region
(400 um diameter)
Top view
1:20 scale (1mm = 2 cm in diagram)

## Slide 14
VISAR
Streak camera
VISAR
Streak camera
532 nm laser
532 nm
532 nm
400 -500 nm
Self-emission & reflected 532 nm
SOP streak camera
VULCAN
Dichroic mirror
Beam-splitters
Filters
Experiment schematic

## Slide 15
VISAR
View 2
View 1
Vulcan beam
Shock
Quartz is transparent to VISAR
Foam is opaque to VISAR
View 1
View 2
Time
Measured velocity

## Slide 16
VISAR
Vulcan beam
Shock
View 1
View 2
Time
Measured velocity
Quartz is transparent to VISAR
Foam is opaque to VISAR
View 2
View 1

## Slide 17
VISAR
Vulcan beam
Shock
View 1
View 2
Time
Measured velocity
Shock front in quartz is reflective
Foam is still opaque
View 2
View 1
= shock enters quartz

## Slide 18
VISAR
Vulcan beam
Shock
View 1
View 2
Time
Measured velocity
View 2 signal expires when shock leaves quartz
View 1 still cannot see the shock
View 2
View 1
= shock enters quartz
= shock leaves quartz, enters foam

## Slide 19
VISAR
Vulcan beam
Shock
View 1
View 2
Time
Measured velocity
View 1 also expires when the shock leaves the foam
= shock enters quartz
= shock leaves quartz, enters foam
= shock leaves foam
View 2
View 1

## Slide 20
VISAR data (not yet published)

## Slide 21
MC analysis for error quantification

## Slide 22
Results (not yet published)

## Slide 23
Comparison with simulation
2D flash simulation of the target
Simulated transit times compared to experimental data (Hyades, Helios, Multi, Multi-2d, Flash 1D + 2D)

## Slide 24
Summary
We performed an experiment to measure the principle Hugoniot of TMPTA foam relevant to hydrodynamic equivalent ICF capsules, based around the principle of impedance matching.
Our results suggest that this material can be reasonably well described by the equation of state for low-density homogenous plastic.

## Slide 25
Acknowledgements
Many thanks to everyone involved in the experiment, including all our collaborators at Oxford, York, LULI, ENEA, IPPLM, GSI, FUB, CLF, AWE.
Thanks to the experimental staff at the CLF for their assistance.
Thanks to UKRI-STFC, UKRI-EPSRC, and AWE for funding.

## Slide 26
Experimental comparison