## Slide 1: Boundaries for R&D of HTS-CS Conductor 2021-2024
P. Bruzzone
14 April 2021

## Slide 2: Aim of the R&D
In the pre-conceptual phase of EUROfusion DEMO, two designs are proposed for the CS modules:
1. a hybrid design by double-layers of HTS, R&W Nb3Sn and NbTi
2. an ITER like W&R Nb3Sn by multi-pancakes
The down selection will be done in late 2024 based on the achievements of the activities on both designs.
For the innovative design 1, the R&D for the HTS conductor grade is critical.
A demonstration of feasibility for a high current, no degradation, stable DC performance HTS conductor is mandatory to have design 1 selected in 2024.

## Slide 3: Target range of operation - 4.5 K, 18 T, 60 kA, 1.5 m
The candidate will be a forced flow conductor cooled by supercritical helium flow with inlet temperature 4.5 K, inlet pressure 6 bar and pressure drop 1 bar (same as all other conductors and coils of DEMO).
The peak operating field is set at 18 T (in the latest design options the field ranges between 17.5 T and 18.5 T).
The target operating current is at 60 kA. In former CS design Iop was ≈ 48 kA, but an increase of Iop is desirable to avoid an inductance much higher than ITER and limit the voltage at the plasma start up.
The inner radius of the CS modules is the tightest bending radius for the HTS high grade conductor, Rb = 1.5 m.

## Slide 4: Other design requirements
As for any CS conductor, the AC loss and heat removal are important features. Presently, no quantitative limit is set for time constant. The designer must aim for tolerably low AC loss. As soon as experimental results on prototype AC loss will be available, a thermal-hydraulic assessment will be done and corrective actions may be taken.
The short length prototypes in this phase may be prepared either by industrial machinery or on laboratory scale. In any case, a realistic, affordable projection for long length manufacture must be described in the design.

## Slide 5: Preliminary R&D – Full size
Depending on the maturity (former experience) of the proposed design, preliminary trials may be required before finalizing the conductor layout. The trials must be carried out within a time frame consistent with a full size test latest by early 2024.
The full size test in SULTAN lasts 2-3 weeks and addresses the DC performance (retention of tape performance in cable and performance stability over cyclic loading and WUCD) and the transient loss. The test in SULTAN is complemented by steady state AC loss at Un. Twente.

## Slide 6: Tentative Organization
To increase the chances of success, several prototypes should be developed in parallel, e.g. two SULTAN samples (= four conductors). If enough proposals are presented, the number of SULTAN samples can be increased to three (=six conductors).
Within next month, each proposal should be completed with the list and schedule of the critical R&D steps, milestones for key procurement.
A monitoring meeting will be held every second month to present progress, feedback on design, update of schedule. The detailed organization will be finalized after this meeting.