## Slide 1: ASTRA conductor for DEMO CS
N. Bykovskiy
D. Uglietti
P. Bruzzone
R. Wesche
X. Sarasola
K. Sedlak
13 April 2021

## Slide 2: Design considerations
Strand design:
  Rectangular profile, rounded corners
  Open soldering channel
  Non-twisted soldered tapes
Cable design:
  Roebel cabling
  Jacket pre-compression
  Separate cooling channel
ASTRA (Aligned Stacks Transposed in Roebel Arrangement) conductor features:
  Simplified and well controlled strand soldering
  Favorable direction of transverse load (compression along c-axis)
  Aligned stacks, thus less tapes needed (~50% in central modules, for details see last slide)
  Reduced AC losses (less strands needed)
  Conduction cooling conditions to address fatigue issues of DEMO CS
Field
Force
Current
Mechanical issue with unsupported strand section…
Likely, the key aspects to avoid cyclic load degradation

## Slide 3: Proposed design solutions
Short transition of strands between the cable layers
Impregnation of the cable space
reduced cable thickness (no core), min bending radius <1.5 m
Profile annealing
Strand pre-shape (easy bending)
Strand soldering
Strand cabling (hard bending)
* Tape packing before or after 2.

## Slide 4: Proposed design solutions
Short transition of strands between the cable layers
Impregnation of the cable space
Various filling options to be investigated (only the mechanical reason):
Glycerin + water (aiming at reduced thermal expansion)
Paraffin wax (melting point ~50oC)
… Nitrogen?
LN2 first trials
In-field test
Forced flow helium
Liquid impregnation
reduced cable thickness (no core), min bending radius <1.5 m
 Related study from 1975…
https://doi.org/10.1016/0011-2275(75)90034-X

## Slide 5: Sub-scale ASTRA sample for quench experiment
QE sample features:
Operation in parallel DC field
Conduction cooling
Electrically insulated and thermally coupled MgB2 wire in highly resistive matrix for early quench detection
Co-wound SC wire vs fiber optics:
Cheaper, simplified and more robust instrumentation
Location of hot-spot can not be identified
Co-wound SC wire vs voltage taps:
Increased sensitivity of voltage detection (~100 times at low T)
Reparability is the main issue (similar to co-wound voltage taps)

## Slide 6: Action items towards performance demonstration
Test SULTAN sample
Short transition of strands
Long-length strand soldering
Cabling
Conduction cooling
Conductor terminations
Integration and instrumentation
Liquid impregnation
New QE sample
Material procurement
SST 3.3 mm tapes: completed
Copper profiles: small (required) amount ordered
Cooling channel: follow-up QE sample
Protection copper: TBD
Steel and copper components: TBD
Time and amount of tape needed
~2 months ~20 m
~4 months ~10 m
~6 months ~80 m
~10 months ~300 m
Conductor performance assessment
Discussion
SST tapes characterization

## Slide 7: DEMO CS coils: tapes needed for ASTRA conductor
Dashed lines: tapes aligned along z-axis
Solid lines: ± 5 deg mismatch with z-axis
3.3 mm SST tapes
CS module | CS3L | CS2L | CS1 | CS2U | CS3U
Most demanding operating conditions | PREMAG: 14.66 T / 70.1o | EOF: 12.59 T / 70.1o | PREMAG: 18.14 T / 83.7o | EOF: 13.16 T / 70.3o | PREMAG: 15.03 T / 70.2o
~330 tapes (SST 3.3 mm) needed for the operation in perpendicular peak field