## Slide 1: T-01-01 Tasks for R&D of HTS-CS Conductor
P. Bruzzone
11 May 2021

## Slide 2: From the meeting on April 13th 2021
Three RU’s (ENEA, KIT and SPC) have expressed interest to develop and assemble prototype conductors for the innermost layer of the hybrid DEMO CS.
“Within next month, each proposal should be completed with the list and schedule of the critical R&D steps, milestones for key procurement.”
The various prototypes will be paired in 2-3 SULTAN samples.
The test of the prototypes in SULTAN must be completed by early 2024.
The detailed task specifications (T-01-01) are being agreed with the PL.

## Slide 3: Target range of operation - 4.5 K, 18 T, 60 kA, 1.5 m
The prototype is a forced flow conductor cooled by supercritical helium flow with inlet temperature 4.5 K, inlet pressure 6 bar and pressure drop 1 bar (same as all other conductors and coils of DEMO).
The peak operating field is set at 18 T (in the latest design options the field ranges between 17.5 T and 18.5 T).
The target operating current is at 60 kA. Over-current may be applied in the SULTAN test to reproduce the actual electromagnetic loads
The inner radius of the CS modules is the tightest bending radius for the HTS high grade conductor, Rb = 1.5 m.

## Slide 4: Key requirements
The SULTAN test will verify the key requirement of the DC performance. The target is to retain the DC performance of the free standing tape (measured in field at low temperature). The DC performance must remain stable under at least 5000 em loads and two thermal cycles. The requirement of bending on Rb = 1.5m will be experimentally verified by bending/straightening the conductor before the test in SULTAN. A test “as bent at Rb = 1.5m” can also be carried out at liquid nitrogen self-field
AC loss will be measured in SULTAN for sinusoidal and trapezoidal field – if necessary the orientation of the AC field can be rotated by 90º. For non-twisted stacks, the AC loss test in SULTAN is drastically underestimating the coupling currents loss, i.e. the test in SULTAN is not conclusive for AC loss.
The heat generation/removal and the peak temperature in operation with the reference scenario will be assessed by a thermal-hydraulic analysis taking as input the winding pack geometry (TBD), the measured DC performance and the (guessed) AC loss.

## Slide 5: Test in SULTAN
The conductor should be applicable at any of the CS modules, disregarding the field-conductor angle – the path to termination must also be accounted.
As the sample in SULTAN has a specific field orientation, the prototypes with non-twisted tapes may have a different performance in SULTAN compared to real CS. Each designer must provide the expected performance for both SULTAN test and CS operation.
The em load in SULTAN should match the actual em load in CS, e.g. by applying at 11T a 98kA current (11·98 = 18·60). The relevance of the load orientation must be discussed.

## Slide 6: Tentative Organization
Each prototype has a “speaker” responsible to report periodically the progress (and any issue) to the technology coordinator (PB) and project leader (VC).
At the end of each month, the speakers send an email message (or a one page summary) about the status and progress.
Every three months, a video meeting is held to summarize the progress and coordinate the schedule in a sort of technical meeting.