## Slide 1: ENEA contribution to the R&D of HTS conductors
Zoom Meeting, 2021/05/11
Hybrid HTS/LTS CS within F9-WPMAG

## Slide 2: HTS slotted-core for CS DEMO insert coil
ENEA  study an alternative conceptual design of an HTS + LTS hybrid CS DEMO system based on:
- REBCO tapes, with Al-slotted core conductor technology.
- BiSCCO. At least in the first stage, we will consider an alternative based on it.

## Slide 3: HTS slotted-core for CS DEMO insert coil
Issues to be addressed…
slots:
  are useful for direct cooling?;
  filled with thermal/mechanical effective fillers?;
HTS stack:
  Additional mechanical support to sustain em loads is necessary?;
  Soldered? A reliable W&R process must be developed to take advantage from the more mechanical tolerant “slipping-tape” configuration during manufacturing and winding;
Jacket:
  Aluminum (high strength Al-alloy) preferable for thermal property matching with core;
  SS preferable in a perspective of long length cable production (can be welded, for Al welding is an issue)
  Round / Cicle-in-square?
We expect some of these concerns could be clarified by the results of quench conductor test
Al slotted-core conductor (basic technological features: Al core extrusion + HTS tape stack)
Where we are:
A lot of practical / handling issues already experienced;
many experimental evidences accumulated;
What we need to do:
performance verification in a fully equipped sample and under relevant electromagnetic load conditions still to be assessed.

## Slide 4: HTS slotted-core for CS DEMO insert coil
Target range of operation
Inlet Temperature = 4.5 K,
Peak field = 18 T,
Operating current = 60 kA,
Bending radius = 1.5 m
P. Bruzzone ” Boundaries for R&D of HTS-CS Conductor 2021-2024” Meeting WPMAG 13/04/2021
A. Molodyk, et al., Sci. Rep. (2021) 11:2084
commercial production grade
Similar for Bi-2223  about 300+
Based on typical performances  about 300+ YBCO HTS tapes

## Slide 5: HTS slotted-core for CS DEMO insert coil
Al slotted-core with 10 Slots
10 HTS stacks x 30 tapes
Pros
- Assessed manufacturing process
- High Je
Contras
- Manufacturing complexity due to huge number of tapes/stacks
- Concerns on minimum bending radius (?)

## Slide 6: HTS slotted-core for CS DEMO insert coil
Al slotted-core with 10 Slots
10 HTS stacks x 30 tapes
Advanced cooling layout
Developed for the 6 slots core. To be tested in the next quench experiment @ SULTAN
Core cooling dual path
Core Center (channel);
Core Periphery (6 grooves);
 More uniform cooling mechanism
If successful, it will be adopted to the 10 slot layout

## Slide 7: Alternative layout of a HTS slotted-core
Flat cable
(Untwisted) Al slotted-core with 6 Slots
6 x 30 HTS tapes
Pros
Reduced number of HTS tapes (a factor 2+ with respect to twisted)
higher aspect ratio cable can be envisaged (thinner & more # stacks)
More tolerant configuration against bending loads
Appealing for Bi-2223 tapes
Contras
Tolerable Δr to be defined
New cabling concept to be fully developed and assessed
Cooling channel
H
Δr
Δr = 10 mm  6 cm of max tape extra length (Rcoil = 1.5 m)

## Slide 8: Alternative layout of a HTS slotted-core
Round Dual Stack Macro-strand
Al slotted-core with 2 Slots
2 x 30 HTS tapes
Tentative conductor layout for a 60 kA, high field operation
5 strands x 60 HTS = 300 tapes
Pros
- Macro-strand easier to manufacture/handle
Contras
- New cabling concept to be fully developed and assessed
- Very similar to other already proposed approaches based on round strands by SPC and KIT
Cooling channel
Jacketed/wrapped strands
31.5 mm
fillers
Main drivers:
easier manufacturing;
more friendly handling;
Investigation of new cable concept/layout

## Slide 9: Alternative layout of a HTS slotted-core
Main drivers:
easier manufacturing;
more friendly handling;
Investigation of new cable concept/layout
Inspired by sector conductor approach aimed at minimizing the cable diameter
Single stack Macro-Strand for HTS sector cable
Al slotted-core for one HTS stack
1 x 40/50 HTS tapes
taken from Google…
Two base elements 
Macro-Strand
+
Central support

## Slide 10: Time schedule
- Definition of a proper conductor layout
- Material procurements
- Investigation and assessment of manufacturing / layout details: experimental campaign on short/sub-size samples
- SULTAN sample manufacturing
- Performance tests @ SULTAN
Sept./Oct. 2021
Dec. 2021
Mar./Apr. 2022
Sept./Oct. 2022
Dec. 2022 (?)

## Slide 11: Alternative layout of a HTS slotted-core
Single stack Macro-Strand for sectorial cable approach
Al slotted-core with 1 Slots
1 x 40/50 HTS tapes
Main drivers:
easier manufacturing;
more friendly handling;
Investigation of new cable concept/layout