## Slide 1: DTT Central Solenoid design status
L . Muzzi
ENEA FSN-COND
DTT CTS Meeting ; 24/25-07-2023
DTT Consortium (DTT S.C.a r.l. Via E. Fermi 45 I-00044 Frascati (Roma) Italy)

## Slide 2: Features of the DTT CS coil
L. Muzzi – ENEA FSN COND – 24/07/2023
RECAP:
«non-standard» layer-wound coil necessary, to provide:
Due to geometrical constraints and physics requirements:
Winding pack current density: JENG: 30 – 40 A/mm2

## Slide 3: Central Solenoid Coils design status
Presently, a 2-grades, layer-wound coil solution is the reference.
 | Layer – 2 Grades_V04_R00
Winding pack layout | 6 layers x 18 turns (HF section) 6 layers x 27 turns (LF section)
CICC operating current | 34 kA
# s.c. / Cu strands in CICC | 768 / 0 (HF); 168 / 228 (LF)
CICC dimensions (non-insulated) | 42.0 mm x 27.7 mm (HF) 27.3 mm x 19.3 mm (LF)
Jacket thickness | 4.55 mm (HF) / 2.56 mm (LF)
Turn insulation | 1 mm
CICC length per CS module | 361 m (HF) + 699 m (LF)
Winding pack dimensions | 315 mm x 800 mm
Coil inner radius | 441 mm
Module self-inductance | 66 mH
Inter-module axial spacer | 64 mm
Winding features | 1 inter-module external joint + 2 terminations; 6 He inlets and 8 He outlets
Hydraulic length | between 52 m and 69 m (HF) between 107 m and 126 m (LF)
Max. Volt. @ breakdown | 2.8 kV
Max. inter-turn volt. | 640 V (between layers 11 and 12)
Ideal / Real Magnetic Flux | 17.0 / 16.2 Weber
30.9 x 15.6 mm
44.5 x 28.3 mm
HF
LF
L. Muzzi – ENEA FSN COND – 24/07/2023

## Slide 4: Central Solenoid Coils design: open issues
Issue 1: we have to rely on heat-treatment tolerant insulation (glass+VPI) only, and the insulation is highly loaded mechanically;
L. Muzzi – ENEA FSN COND – 24/07/2023
Issue 2: Thermo-hydraulic configuration is not optimal (cold He does not directly enter at the coil high-field region);
Issue 3: the procurement of the Nb3Sn strand has to be launched again, and the performance brought back to the “original request”:
Ic(4.2K-12T) > 260 A (about 8% lower)
Hyst. Loss < 400 mJ/cm3
Issue 4: Distribution of the pre-compression load on the two sub-coils with different stiffness could be “tricky”. To be still studied and assessed.
Issue 5: Same comment as above concerning quench detection strategy.

## Slide 5: Central Solenoid Coils design: open issues
Issue 1: we have to rely on heat-treatment tolerant insulation (glass+VPI) only, and the insulation is highly loaded mechanically;
L. Muzzi – ENEA FSN COND – 24/07/2023

## Slide 6: Central Solenoid Coils design: open issues
Issue 1: we have to rely on heat-treatment tolerant insulation (glass+VPI) only, and the insulation is highly loaded mechanically;
L. Muzzi – ENEA FSN COND – 24/07/2023
«Standard» mechanical criteria for insulation components are not satisfied

## Slide 7: Central Solenoid Coils design: open issues
Issue 1: we have to rely on heat-treatment tolerant insulation (glass+VPI) only, and the insulation is highly loaded mechanically;
L. Muzzi – ENEA FSN COND – 24/07/2023
«Standard» mechanical criteria for insulation components are not satisfied
CS1U turn insulation. Regions exceeding the LHD criterion

## Slide 8: Central Solenoid Coils design: open issues
Issue 1: we have to rely on heat-treatment tolerant insulation (glass+VPI) only, and the insulation is highly loaded mechanically;
L. Muzzi – ENEA FSN COND – 24/07/2023
«Standard» mechanical criteria for insulation components are not satisfied
CS1U turn insulation. Regions exceeding the LHD criterion
So, what happens during machine lifetime?

## Slide 9: Central Solenoid Coils design: open issues
Issue 1: we have to rely on heat-treatment tolerant insulation (glass+VPI) only, and the insulation is highly loaded mechanically;
L. Muzzi – ENEA FSN COND – 24/07/2023
«Standard» mechanical criteria for insulation components are not satisfied
CS1U turn insulation. Regions exceeding the LHD criterion
Max. terminal-to-terminal voltage (at breakdown): 2.8 kV
Max. inter-turn voltage (at breakdown): 640 V
So, what happens during machine lifetime?
Can we guarantee the capability to maintain:
(between two outermost LF layers, 11 and 12; 360 V between outermost HF layers, 5 and 6)

## Slide 10: Central Solenoid Coils design: open issues
Issue 1: we have to rely on heat-treatment tolerant insulation (glass+VPI) only, and the insulation is highly loaded mechanically;
L. Muzzi – ENEA FSN COND – 24/07/2023
«Standard» mechanical criteria for insulation components are not satisfied
Terminal-to-terminal voltage to be treated with «common practice»; but for the inter-turn insulation:
risk mitigation strategy, based on two main points:
further optimization of scenarios, aimed at a reduction of mechanical loads
Manufacture and integrated electro-mechanical test of an insulation mock-up

## Slide 11: Central Solenoid Coils design: open issues
Issue 1: we have to rely on heat-treatment tolerant insulation (glass+VPI) only, and the insulation is highly loaded mechanically;
L. Muzzi – ENEA FSN COND – 24/07/2023
«Standard» mechanical criteria for insulation components are not satisfied
Terminal-to-terminal voltage to be treated with «common practice»; but for the inter-turn insulation:
risk mitigation strategy, based on two main points:
further optimization of scenarios, aimed at a reduction of mechanical loads
Manufacture and integrated electro-mechanical test of an insulation mock-up

## Slide 12: Winding Pack Electrical Insulation
DTT CS Design Update Meeting
L. Muzzi – ENEA FSN COND – 24/07/2023
Manufacture of two 5 x 5 mock-ups (a HF- and a LF-relevant one), about 0.5 m long, employing the full process (sand-blasting; glass wrapping; assembly; heat treatment; VPI; 4 mm ground insulation application);
Application at 77 K of a mechanical compression load
Electrical tests layout (see later)

## Slide 13: Winding Pack Electrical Insulation
DTT CS Design Update Meeting
L. Muzzi – ENEA FSN COND – 24/07/2023
Effect of 390 tons compressive load on LF
Effect of 640 tons compressive load on HF
Computed stress in operation
Manufacture of two 5 x 5 mock-ups (a HF- and a LF-relevant one), about 0.5 m long, employing the full process (sand-blasting; glass wrapping; assembly; heat treatment; VPI; 4 mm ground insulation application);
Application at 77 K of a mechanical compression load that provides a stress equivalent to the one computed in operation;

## Slide 14: Winding Pack Electrical Insulation
DTT CS Design Update Meeting
L. Muzzi – ENEA FSN COND – 24/07/2023
Acceptance criteria:
Electrical insulation maintained for an applied voltage level (between central turn and any of the adjacent ones):
   1500 V / 850 V, in LF / HF mock-up, respectively
Max. inter-turn voltage computations:
- 640 V for LF CICC (between L12 ed L11);
- 360 V for HF CICC (between L5 and L6).
Manufacture of two 5 x 5 mock-ups (a HF- and a LF-relevant one), about 0.5 m long, employing the full process (sand-blasting; glass wrapping; assembly; heat treatment; VPI; 4 mm ground insulation application);
Application at 77 K of a mechanical compression load that provides a stress equivalent to the one computed in operation;
Measurement of the inter-turn electrical insulation, before and after the cyclic (up to 25000?) application of load.

## Slide 15: Winding Pack Electrical Insulation
DTT CS Design Update Meeting
L. Muzzi – ENEA FSN COND – 24/07/2023
Acceptance criteria:
Electrical insulation maintained for an applied voltage level (between central turn and any of the adjacent ones):
   1500 V / 850 V, in LF / HF mock-up, respectively
Max. inter-turn voltage computations:
- 640 V for LF CICC (between L12 ed L11);
- 360 V for HF CICC (between L5 and L6).
Manufacture of two 5 x 5 mock-ups (a HF- and a LF-relevant one), about 0.5 m long, employing the full process (sand-blasting; glass wrapping; assembly; heat treatment; VPI; 4 mm ground insulation application);
Application at 77 K of a mechanical compression load that provides a stress equivalent to the one computed in operation;
Measurement of the inter-turn electrical insulation, before and after the cyclic (up to 25000?) application of load.
Discussion is also on-going, to verify the possibility of manufacturing and testing an additional mock-up made with Mica, instead of glass tape

## Slide 16: Central Solenoid Coils design: open issues
Issue 2: Thermo-hydraulic configuration is not optimal (cold He does not directly enter at the coil high-field region);
L. Muzzi – ENEA FSN COND – 24/07/2023
Issue 3: the procurement of the Nb3Sn strand has to be launched again, and the performance downgraded back to the “original request”:
Ic(4.2K-12T) > 260 A (about 8% lower)
Hyst. Loss < 400 mJ/cm3

## Slide 17: CS Coil Thermal-hydraulics
L. Muzzi – ENEA FSN COND – 24/07/2023
Temperature margin (min. DTmargin) verified for the layer-wound CS coil, with original strand properties: Ic (@ ref. conditions) > 260 A; Hyst. Losses (+/- 3 T) < 400 mJ/cm3
At EoF – Scenario v14i1 (scaled with max curr, e.g., 34 kA for layer-wound)

## Slide 18: CS Coil Thermal-hydraulics
Temperature margin (min. DTmargin) verified for the layer-wound CS coil, with original strand properties: Ic (@ ref. conditions) > 260 A; Hyst. Losses (+/- 3 T) < 400 mJ/cm3
At EoF – Scenario v14i1 (scaled with max curr, e.g., 34 kA for layer-wound)
Options to «recover» temperature margin?
Further coil design review, adapted to the original strand performance  most likely leading to a magnetic flux decrease (maybe a few tenths of Vs?)
Sub-cooling of supercritical helium, to 4.2 K (0.3 K less than currently considered as a reference);
Increase of CS current ramp-up time; introduction of a current plateau after reaching Initial Magnetization, to get rid of the heat accumulated during the current ramp
L. Muzzi – ENEA FSN COND – 24/07/2023

## Slide 19: CS Coil Thermal-hydraulics
Temperature margin (min. DTmargin) verified for the layer-wound CS coil, with original strand properties: Ic (@ ref. conditions) > 260 A; Hyst. Losses (+/- 3 T) < 400 mJ/cm3
At EoF – Scenario v14i1 (scaled with max curr, e.g., 34 kA for layer-wound)
Options to «recover» temperature margin?
Further coil design review, adapted to the original strand performance  most likely leading to a magnetic flux decrease;
Sub-cooling of supercritical helium, to 4.2 K (0.3 K less than currently considered as a reference);
Increase of CS current ramp-up time; introduction of a current plateau after reaching Initial Magnetization, to get rid of the heat accumulated during the current ramp
L. Muzzi – ENEA FSN COND – 24/07/2023

## Slide 20: CS Coil Thermal-hydraulics
Temperature margin (min. DTmargin) verified for the layer-wound CS coil, with original strand properties: Ic (@ ref. conditions) > 260 A; Hyst. Losses (+/- 3 T) < 400 mJ/cm3
At EoF – Scenario v14i1 (scaled with max curr, e.g., 34 kA for layer-wound)
Options to «recover» temperature margin?
L. Muzzi – ENEA FSN COND – 24/07/2023
NOTE: He transit time through the 52 m of innermost HF turn = 210 s

## Slide 21: CS Coil Thermal-hydraulics
Temperature margin (min. DTmargin) verified for the layer-wound CS coil, with original strand properties: Ic (@ ref. conditions) > 260 A; Hyst. Losses (+/- 3 T) < 400 mJ/cm3
At EoF – Scenario v14i1 (scaled with max curr, e.g., 34 kA for layer-wound)
Options to «recover» temperature margin?
Further coil design review, adapted to the original strand performance  most likely leading to a magnetic flux decrease;
Sub-cooling of supercritical helium, to 4.2 K (0.3 K less than currently considered as a reference);
Increase of CS current ramp-up time; introduction of a current plateau after reaching Initial Magnetization, to get rid of the heat accumulated during the current ramp
Different cooling layout: He inlet at the center of the innermost layer, thus halving the hydraulic path of the most loaded, highest field, innermost layer.
L. Muzzi – ENEA FSN COND – 24/07/2023

## Slide 22: CS Coil Thermal-hydraulics
L. Muzzi – ENEA FSN COND – 24/07/2023
Currently assumed cooling layout for layer-wound coil (6 + 6 layers)
Hydraulic length of innermost HF layer = 52 m
Cold He inlet
«Hot» He outlet
Conductor Termination

## Slide 23: CS Coil Thermal-hydraulics
L. Muzzi – ENEA FSN COND – 24/07/2023
Currently assumed cooling layout for layer-wound coil (6 + 6 layers)
Hydraulic length of innermost HF layer = 52 m
Alternative cooling He inlet and outlets
Hydraulic length of innermost HF layer = 26 m

## Slide 24: CS Coil Thermal-hydraulics
L. Muzzi – ENEA FSN COND – 24/07/2023
Currently assumed cooling layout for layer-wound coil (6 + 6 layers)
Hydraulic length of innermost HF layer = 52 m
Alternative cooling He inlet and outlets
Hydraulic length of innermost HF layer = 26 m
... BUT:

## Slide 25: CS Coil Thermal-hydraulics
L. Muzzi – ENEA FSN COND – 24/07/2023
Currently assumed cooling layout for layer-wound coil (6 + 6 layers)
Hydraulic length of innermost HF layer = 52 m
Alternative cooling He inlet and outlets
Hydraulic length of innermost HF layer = 26 m
... BUT:
He inlet at inter-layer joint to be avoided!

## Slide 26: CS Coil Thermal-hydraulics
L. Muzzi – ENEA FSN COND – 24/07/2023
Coil Winding should be changed, to accomodate an odd number of layers.
The layout would thus schematically appear as:
1st HF termination exiting on one coil side; 2nd HF termination and both LF terminations on the other side

## Slide 27: CS Coil Thermal-hydraulics
Temperature margin (min. DTmargin) verified for the layer-wound CS coil, with original strand properties: Ic (@ ref. conditions) > 260 A; Hyst. Losses (+/- 3 T) < 400 mJ/cm3
At EoF – Scenario v14i1 (scaled with max curr, e.g., 34 kA for layer-wound)
Options to «recover» temperature margin?
Further coil design review, adapted to the original strand performance  most likely leading to a magnetic flux decrease;
Sub-cooling of supercritical helium, to 4.2 K (0.3 K less than currently considered as a reference);
Increase of CS current ramp-up time; introduction of a current plateau after reaching Initial Magnetization, to get rid of the heat accumulated during the current ramp
Different cooling layout: He inlet at the center of the innermost layer, thus halving the hydraulic path of the most loaded, highest field, innermost layer.
L. Muzzi – ENEA FSN COND – 24/07/2023
NOTE: a +/- 30% uncertainty should be considered on computed AC Losses

## Slide 28: Central Solenoid Coils design: open issues
Issue 4: Distribution of the pre-compression load on the two sub-coils with different stiffness could be “tricky”. Still to be studied and assessed.
Issue 5: Same comment as above, concerning quench detection strategy. Still to be studied and assessed.
L. Muzzi – ENEA FSN COND – 24/07/2023

## Slide 29: Alternative pancake-wound solution
An alternative pancake-wound option is being considered as well, but not satisfying the physics requirements.
1 inter-pancake joint ; Iop = 31.0 kA;
Top = 4.8 K (Top = 6.2 K in layer-wound coil)
Peak inter-turn insulation is smaller than in the layer-wound;
Axial mechanical loads better distributed on this geometry.
BUT some risks identified in the handling of the innermost turn after Nb3Sn H.T.
L. Muzzi – ENEA FSN COND – 24/07/2023
 | Pancake –N_05_R00
Winding pack layout | 28 pancakes, with 10 turns each
CICC operating current | 31 kA
# s.c. / Cu strands in CICC | 300 / 129
CICC dimensions (non-insulated) | 27.4 mm x 25.3 mm
Jacket thickness | 3.75 mm
Turn insulation | 1 mm
CICC length per CS module | 2 x 545 m
Winding pack dimensions | 281 mm x 830 mm
Coil inner radius | 479 mm
Module self-inductance | 69 mH
Inter-module axial spacer | 10 mm
Winding features | 1 inter-pancake joint + 2 terminations; 14 He inlets and 15 outlets
Hydraulic length | 39 m
Max. Volt. @ breakdown | 2.7 kV
Max. inter-turn volt. | 195 V (between pancakes 14 and 15)
Ideal / Real Magnetic Flux | 15.9 / 15.6 Weber

## Slide 30: Alternative pancake-wound solution
An alternative pancake-wound option is being considered as well, but not satisfying the physics requirements.
Peak inter-turn insulation is smaller than in the layer-wound;
Axial mechanical loads better distributed on this geometry.
BUT some risks identified in the handling of the innermost turn after Nb3Sn H.T.
Min. DTmargin not influenced by current scenario
L. Muzzi – ENEA FSN COND – 24/07/2023
To be re-computed with downgraded wire performance
1 inter-pancake joint ; Iop = 31.0 kA;
Top = 4.8 K (Top = 6.2 K in layer-wound coil)

## Slide 31: Concluding remarks
L. Muzzi – ENEA FSN COND – 24/07/2023
The design of the DTT Central Solenoid (CS) coil has proven to be challenging.
Concerns on the integrity of the electrical insulation throughout the machine lifetime. Beside the “normally-adopted” criteria for insulation assessment, a relevant mock-up test will be used for design assessment and acceptance.
A layer-wound, 2-grades coil solution, operating at 34 kA, and providing an (ideal) 17.0 Weber flux still represents the baseline, but a pancake-wound one has been designed as well, providing (ideal) 15.9 Weber.
But “downgraded” wire performance call for a re-assessment of all numbers. A re-design activity will be necessary, to “recover” the minimum required temperature margin.
Some analyses (mechanical and thermo-hydraulic) need still be carried out, and no systematic fault analysis has been undertaken.
Quench detection and coil protection strategy is still to be developed. Quench detection is more difficult in layer-wound coil solutions.
Some optimization on the current scenarios is being attempted to reduce loads.